401 GRANULAR SUB-BASE

401.1 Scope

This work shall consist of laying and compacting well-graded material on prepared subgrade

in accordance with the requirements of these Specifications. The material shall be laid in

one or more layers as sub-base or lower sub-base and upper sub-base (termed as subbase

hereinafter) as necessary according to lines, grades and cross-sections shown on the

drawings or as directed by the Engineer.

401.2 Materials

401.2.1 The material to be used for the work shall be natural sand, crushed gravel,

crushed stone, crushed slag, or combination thereof depending upon the grading required.

Use of materials like brick metal, Kankar and crushed concrete shall be permitted in the lower

sub-base. The material shall be free from organic or other deleterious constituents and shall

conform to the gradings given in Table 400-1 and physical requirements given in Table 400-2.

Gradings III and IV shall preferably be used in lower sub-base. Gradings V and VI shall be

used as a sub-base-cum-drainage layer. The grading to be adopted for a project shall be as

specified in the Contract. Where the sub-base is laid in two layers as upper sub-base and

lower sub-base, the thickness of each layer shall not be less than 150 mm.

401.2.2 If the water absorption of the aggregates determined as per IS:2386

(Part 3) is greater than 2 percent, the aggregates shall be tested for Wet Aggregate Impact

Value (AIV) (IS:5640). Soft aggregates like Kankar, brick ballast and laterite shall also be

tested for Wet AIV (IS:5640).

Table 400-1 : Grading for Granular Sub-base Materials

IS Sieve

Designation

Percent by Weight Passing the IS Sieve

Grading I Grading II Grading III Grading IV Grading V Grading VI

75.0 mm 100 - - - 100 -

53.0 mm 80-100 100 100 100 80-100 100

26.5 mm 55 –90 70-100 55-75 50-80 55-90 75-100

9.50 mm 35-65 50-80 – – 35-65 55-75

4.75 mm 25 – 55 40-65 10-30 15-35 25-50 30-55

2.36 mm 20- 40 30-50 – – 10-20 10-25

0.85 mm – – – – 2-10 –

0.425 mm 10-15 10- 15 – – 0-5 0-8

0.075 mm <5 < 5 < 5 < 5 – 0-3

Section 400 Sub-Bases, Bases (Non-Bituminous) and Shoulders

110

Table 400-2 : Physical Requirements for Materials for Granular Sub-base

Aggregate Impact Value (AIV) IS:2386 (Part 4)

or IS:5640

40 maximum

Liquid Limit IS:2720 (Part 5) Maximum 25

Plasticity Index IS:2720 (Part 5) Maximum 6

CBR at 98% dry density

(at IS:2720-Part 8)

IS:2720 (Part 5) Minimum 30 unless otherwise

specified in the Contract

401.3 Construction Operations

401.3.1 P reparation of Sub-grade

Immediately prior to the laying of sub-base, the subgrade already finished to Clause 301 or

305 as applicable shall be prepared by removing all vegetation and other extraneous matter,

lightly sprinkled with water, if necessary and rolled with two passes of 80–100 kN smooth

wheeled roller.

401.3.2 S preading and Compacting

The sub-base material of the grading specified in the Contract and water shall be mixed

mechanically by a suitable mixer equipped with provision for controlled addition of water

and mechanical mixing. So as to ensure homogenous and uniform mix. The required water

content shall be determined in accordance with IS:2720 (Part 8). The mix shall be spread on

the prepared subgrade with the help of a motor grader of adequate capacity, its blade having

hydraulic controls suitable for initial adjustment and for maintaining the required slope and

grade during the operation, or other means as approved by the Engineer.

Moisture content of the mix shall be checked in accordance with IS:2720 (Part 2) and suitably

adjusted so that, at the time of compaction, it is from 1 to 2 percent below the optimum

moisture content.

Immediately after spreading the mix, rolling shall be done by an approved roller. If the

thickness of the compacted layer does not exceed 100 mm, a smooth wheeled roller of 80 to

100 kN weight may be used. For a compacted single layer upto 200 mm the compaction shall

be done with the help of a vibratory roller of minimum 80 to 100 kN static weight capable of

achieving the required compaction. Rolling shall commence at the lower edge and proceed

towards the upper edge longitudinally for portions having unidirectional cross fall or on super elevation.

For carriageway having cross fall on both sides, rolling shall commence at the

edges and progress towards the crown.

Sub-Bases, Bases (Non-Bituminous) and Shoulders Section 400

111

Each pass of the roller shall uniformly overlap not less than one-third of the track made in the

preceding pass. During rolling, the grade and cross fall (camber) shall be checked and any

high spots or depressions which become apparent, corrected by removing or adding fresh

material. The speed of the roller shall not exceed 5 km per hour.

Rolling shall be continued till the density achieved is at least 98 percent of the maximum

dry density for the material determined as per IS:2720 (Part 8). The surface of any layer

of material on completion of compaction shall be well closed, free from movement under

compaction equipment and from compaction planes, ridges, cracks or loose material. All

loose, segregated or otherwise defective areas shall be made good to the full thickness of

layer and re-compacted.

401.4 S urface Finish and Quality Control of Work

The surface finish of construction shall conform to the requirements of Clause 902. Control

on the quality of materials and works shall be exercised by the Engineer in accordance with

Section 900.

401.5 Arrangements for Traffic

During the period of construction, arrangements for the traffic shall be provided and maintained

in accordance with Clause 112.

401.6 Measurements for Payment

Granular sub-base shall be measured as finished work in position in cubic metres.

The protection of edges of granular sub-base extended over the full formation as shown in

the drawing shall be considered incidental to the work of providing granular sub-base and as

such no extra payment shall be made for the same.

401.7 R ate

The Contract unit rate for granular sub-base shall be payment in full for carrying out the

required operations including full compensation for:

i) making arrangements for traffic to Clause 112 except for initial

treatment to verges, shoulders and construction of diversions;

ii) supplying all materials to be incorporated in the work including all

royalties, fees, rents where applicable with all leads and lifts;

iii) all labour, tools, equipment and incidentals to complete the work to the

Specifications;

iv) carrying out the work in part widths of road where directed; and

v) carrying out the required tests for quality control.

Section 400 Sub-Bases, Bases (Non-Bituminous) and Shoulders

112

402 LIME TREATED SOIL FOR IMPROVED SUB-GRADE/SUB-BASE

402.1 S cope

This work shall consist of laying and compacting an improved sub-grade/lower sub-base of

soil treated with lime on prepared sub-grade in accordance with the requirements of these

Specifications and in conformity with the lines, grades and cross-sections shown on the

drawings or as directed by the Engineer. Lime treatment is generally effective for soils which

contain a relatively high percentage of clay and silty clay.

402.2 Materials

402.2.1 S oil

Except when otherwise specified, the soil used for stabilization shall be the local clayey soil

having a plasticity index greater than 8.

402.2.2 L ime

Lime for lime-soil stabilization work shall be commercial dry lime slaked at site or pre-slaked

lime delivered to the site in suitable packing. Unless otherwise permitted by the Engineer, the

lime shall have purity of not less than 70 percent by weight of Quick-lime (CaO) when tested

in accordance with IS:1514. Lime shall be properly stored to avoid prolonged exposure to the

atmosphere and consequent carbonation which would reduce its binding properties.

402.2.3 Quantity of Lime in Stabilized Mix

Quantity of lime to be added as percentage by weight of the dry soil shall be as specified in

the Contract. The quantity of lime used shall be related to its calcium oxide content which

shall be specified. Where the lime of different calcium oxide content is to be used, its quantity

shall be suitably adjusted with the approval of the Engineer so that equivalent calcium oxide

is incorporated in the work. The mix design shall be done to arrive at the appropriate quantity

of lime to be added, having due regard to the purity of lime, the type of soil, the moisture density

relationship, and the design CBR/Unconfined Compressive Strength (UCS) value

specified in the Contract. The laboratory CBR/UCS value shall be at least 1.5 times the

minimum field value of CBR/UCS stipulated in the Contract.

402.2.4 W ater

The water to be used for lime stabilisation shall be clean and free from injurious substances.

Potable water shall be used.

Sub-Bases, Bases (Non-Bituminous) and Shoulders Section 400

113

402.3 Construction Operations

402.3.1 Weather Limitations

Lime-soil stabilisation shall not be done when the air temperature in the shade is less

than 10ºC.

402.3.2 D egree of Pulverisation

For lime-soil stabilisation, the soil before addition of stabilizer, shall be pulverized using

agricultural implements like disc harrows (only for low volume roads) and rotavators to the

extent that it passes the requirements set out in Table 400-3 when tested in accordance with

the method described in Appendix-3.

Table 400-3 : Soil Pulverisation Requirements for Lime Stabilisation

IS Sieve designation Minimum percent by weight

passing the IS Sieve

26.5 mm 100

5.6 mm 80

402.3.3 E quipment for Construction

Stabilised soil sub-bases shall be constructed by mix-in-place method of construction or as

otherwise approved by the Engineer. Manual mixing shall be permitted only where the width

of laying is not adequate for mechanical operations, as in small-sized jobs.

The equipment used for mix-in-place construction shall be a rotavator or similar approved

equipment capable of pulverizing and mixing the soil with additive and water to specified

degree to the full thickness of the layer being processed, and of achieving the desired degree

of mixing and uniformity of the stabilized material. If so desired by the Engineer, trial runs with

the equipment shall be carried out to establish its suitability for work.

The thickness of any layer to be stabilized shall be not less than 100 mm when compacted. The

maximum thickness can be 200 mm, provided the plant used is accepted by the Engineer.

402.3.4 Mix-in-place Method of Construction

Before deploying the equipment, the soil after it is made free of undesirable vegetation or

other deleterious matter shall be spread uniformly on the prepared subgrade in a quantity

sufficient to achieve the desired compacted thickness of the stabilised layer. Where single-pass

equipment is to be employed, the soil shall be lightly rolled as directed by the Engineer.

Section 400 Sub-Bases, Bases (Non-Bituminous) and Shoulders

114

The equipment used shall either be of single-pass or multiple pass type. The mixers shall be

equipped with an appropriate device for controlling the depth of processing and the mixing

blades shall be maintained or reset periodically so that the correct depth of mixing is obtained

at all times.

With single-pass equipment the forward speed of the machine shall be so selected in relation

to the rotor speed that the required degree of mixing, pulverisation and depth of processing

is obtained. In multiple-pass processing, the prepared sub-grade shall be pulverised to the

required depth with successive passes of the equipment and the moisture content adjusted

to be within prescribed limits mentioned hereinafter. The lime shall then be spread uniformly

and mixing continued with successive passes until the required depth and uniformity of

processing have been obtained.

The mixing equipment shall be so set that it cuts slightly into the edge of the adjoining lane

processed previously so as to ensure that all the material forming a layer has been properly

processed for the full width.

402.3.5 C onstruction with Manual Means

Where manual mixing is permitted, the soil from borrow areas shall first be freed of all

vegetation and other deleterious mater and placed on the prepared subgrade. The soil

shall then be pulverized by means of crow-bars, pick axes or other means approved by the

Engineer.

Water in requisite quantities may be sprinkled on the soil for aiding pulverisation. On the

pulverized soil, the lime in requisite quantities shall be spread uniformly and mixed thoroughly

by working with spades or other similar implements till the whole mass is uniform. After

adjusting the moisture content to be within the limits mentioned later, the mixed material shall

be leveled up to the required thickness so that it is ready to be rolled.

402.3.6 A ddition of Lime

Lime may be mixed with the prepared material either in slurry form or dry state at the option

of the Contractor with the approval of the Engineer.

Dry lime shall be prevented from blowing by adding water to the lime or other suitable means

selected by the Contractor, with the approval of the Engineer.

The tops of windrowed material may be flattened or slightly trenched to receive the lime.

The distance to which lime may be spread upon the prepared material ahead of the mixing

operation shall be determined by the Engineer.

Sub-Bases, Bases (Non-Bituminous) and Shoulders Section 400

115

No traffic other than the mixing equipment shall be allowed to pass over the spread lime until

after completion of mixing.

Mixing or remixing operations, regardless of equipment used, shall continue until the material

is free of any white streaks or pockets of lime and the mixture is uniform.

Non-uniformity of colour reaction, when the treated material is tested with the standard

phenolphthalein alcohol indicator, will be considered evidence of inadequate mixing.

402.3.7 Moisture Content for Compaction

The moisture content at compaction checked vide IS:2720 (Part 2) shall neither be less than

the optimum moisture content corresponding to IS:2720 (Part 8) nor more than 2 percent

above it.

402.3.8 R olling

Immediately after spreading, grading and levelling of the mixed material, compaction shall be

carried out with approved equipment preceded by a few passes of lighter rollers if necessary.

Rolling shall commence at edges and progress towards the centre, except at super elevated

portions or for carriageway with unidirectional cross-fall where it shall commence at the inner

edge and progress towards the outer edge. During rolling, the surface shall be frequently

checked for grade and crossfall (camber) and any irregularities corrected by loosening the

material and removing/adding fresh material. Compaction shall continue until the density

achieved is at least 98 percent of the maximum dry density for the material determined in

accordance with IS:2720 (Part 8).

Care shall be taken to see that the compaction of lime stabilised material is completed within

three hours of its mixing or such shorter period as may be found necessary in dry weather.

During rolling it shall be ensured that roller does not bear directly on hardened or partially

hardened treated material previously laid other than what may be necessary for achieving the

specified compaction at the joint. The final surface shall be well closed, free from movement

under compaction planes, ridges, cracks or loose material. All loose or segregated or otherwise

defective areas shall be made good to the full thickness of the layer and recompacted.

402.3.9 C uring

The sub-base course shall be suitably cured for a minimum period of 7 days after which

subsequent pavement courses shall be laid to prevent the surface from drying out and

becoming friable. No traffic of any kind shall ply over the completed sub-base unless permitted

by the Engineer.

Section 400 Sub-Bases, Bases (Non-Bituminous) and Shoulders

116

402.4 S urface Finish and Quality Control of Work

The surface finish of construction shall conform to the requirements of Clause 902.

Control on the quality of materials and works shall be exercised by the Engineer in accordance

with Section 900.

402.5 Strength

When lime is used for improving the subgrade, the soil-lime mix shall be tested for its CBR

value. When lime stabilized soil is used in a sub-base, it shall be tested for unconfined

compressive strength (UCS) at 7 days. In case of variation from the design CBR/UCS, in situ

value being lower, the pavement design shall be reviewed based on the actual CBR/UCS

values. The extra pavement thickness needed on account of lower CBR/UCS value shall be

constructed by the Contractor at his own cost.

402.6 Arrangements for Traffic

During the period of construction, arrangements for traffic shall be provided and maintained

in accordance with Clause 112.

402.7 Measurements for Payment

Stabilised soil sub-graded sub-base shall be measured as finished work in position in cubic

metres.

402.8 Rate

The Contract unit rate for lime stabilised soil sub-graded/ sub-base shall be payment in full

for carrying out the required operations including full compensation for all components listed

in Clause 401.7 (i) to (v).s